## Slide 1: DoE Neuromorphic Computing Study Group
Stan Williams
Senior Fellow
Hewlett Packard Labs, Palo Alto, CA
October 29, 2015

## Slide 2: Outline
Brief History leading to OSTP Grand Challenge on “Future Computing’ announcement on 10/20
Structure of a Multidisciplinary Neuromorphic Computing Program
    DoE has many, but perhaps not all, of the components for a successful program
After Moore’s transistor shrinking is over, what’s next?
    Look to the brain for clues
    Nonlinear dynamical systems
    Nonvolatile (synaptic) and locally active (neuronic) memristors
Understanding, models and simulation
    Predict the behavior of a nonlinear dynamical system
    Calibrate and validate models
      Electrical test, and physical and chemical characterization
    Microphysical understanding
      High resolution in energy, space and time
Challenge - watching nanoscale devices operate on nanosecond time scales

## Slide 3: A Brief History
US BRAIN Initiative - April 22, 2013
OSTP RFI: “Nanotechnology-Inspired Grand Challenges for the Next Decade” – June 17, 2015
Submitted a response to RFI entitled “Sensible Machines” – June 24
Executive Order: National Strategic Computing Initiative – July 29
Response from OSTP: Sensible Machines shortlisted, asked to ‘develop a program’ – July 30
A flurry of activity! – Aug-Sept
Enlisted the assistance of IEEE Rebooting Computing and ITRS – especially Erik DeBenedictis
Presentation to National Research Council – Sept. 9
Max Planck Society sponsored workshop “Beyond CMOS” – Oct. 7-9
IEEE Non-Volatile Memory Symposium, Beijing – Oct. 12-14
Reviewed Chinese Brain-Inspired Computing Research (CBICR) program – Oct. 15
Tom Kalil announces a new Grand Challenge at NSCI workshop – Oct. 20
“to develop transformational computing capabilities by combining innovations in multiple scientific disciplines”

## Slide 4: URLs for further information
White House announcement of Grand Challenge:
https://www.whitehouse.gov/blog/2015/10/15/nanotechnology-inspired-grand-challenge-future-computing
nano.gov grand challenges portal:
http://www.nano.gov/grandchallenges
IEEE Rebooting Computing Website:
http://rebootingcomputing.ieee.org/archived-articles-and-videos/general/sensible-machine
Sensible Computer White Paper:
http://rebootingcomputing.ieee.org/images/files/pdf/SensibleMachines_v2.5_N_IEEE.pdf

## Slide 6: Moore’s transistor scaling is finally ending
Feature Size
(From Victor Zhirnov, Semiconductor Research Corporation)
14 nm circuits are shipping now
5nm is now viewed as the end of Moore’s law, based on either physics or economics circa 2021!
Challenges in getting below 10 nm: EUV or quadruple exposure immersion patterning
Single monolayer thick active layers inside the devices
Future improvements come from new materials, structures and architectures

## Slide 7: The “Sensible Machine” response to OSTP RFI
The central thesis of this white paper is that although our present understanding of brains is limited, we know enough now to design and build circuits that can accelerate certain computational tasks; and as we learn more about how brains communicate and process information, we will be able to harness that understanding to create a new exponential growth path for computing technology.
I believe this statement much more now than when I first wrote it.

## Slide 8: A model in power efficiency
<25 Watts @ 100 Hz
What are the state variables for communication and computation?
Ion currents and molecular concentrations:
very slow, high energy and inefficient!
How is information processed by an extremely nonlinear dynamical system?
Notes: Apr 2007 Blue Gene /L with 4e3 processors ran a simulation of half a mouse brain (8 million neurons, up to 6300 synapses [no total synapse # provided]) for 10 seconds (only 1 s in the mouse brain).

## Slide 9: Structure of a Neuromorphic Computing Program
Look at existing programs in China: three in Beijing
Peking University
Academia Sinica
Tsinghua University – CBICR program
Operating for three years
35 faculty from seven departments in eight groups
Well conceived, led and funded (internally by Tsinghua)
Already fabbed two chips with a third taped out
Wants to expand program internationally

## Slide 10
Review of CIBCR Tsinghua U.

## Slide 11: Structure of a US Neuromorphic Computing Program
1. Connect Theory of Computation with Neuroscience and Nonlinear Dynamics
e.g. Boolean, CNN, Baysian Inference, Energy-Based Models, Markov Chains
2. Architecture of the Brain and Relation to Computing and Learning
Theories of Mind: Albus, Eliasmith, Grossberg, Mead, many others
3. Simulation of Computational Models and Systems
4. System Software, Algorithms & Apps – Make it Programmable/Adaptable
5. Chip Design – System-on-Chip: Accelerators, Learning and Controllers
Compatible with standard processors, memory and data bus
6. Chip Processing and Integration – Full Service Back End of Line on CMOS
DoE Nanoscale Science Research Centers (NSRCs) – e.g. CINT
7. Devices and Materials – in situ and in operando test and measurement

## Slide 12
Two types of devices (memristors):
Nonvolatile:
‘Synaptic’
State stored as resistance
Continuously variable
Many Examples
ReRAM – vacancies in oxides
PC RAM – Ge-Sb-Te
STT RAM – spins (binary)
Locally Active:
‘Neuronic’ and/or ‘Axonic’
State transmitted as spike
Looks digital
Threshold switching, NDR
Gain, oscillations, chaos
Mott transitions - oxides
Amorphous Ge-Sb-Te

## Slide 13: Memristors have ‘pinched’ hysteresis loops
Nonvolatile Memristor
- Emerging digital memory/storage
- Synapse in neuromorphic circuit
Locally Active (e.g. “Mott”) memristor
- Emerging neuronal compute device
- Passive “selector” in crossbar memories
Leon Chua, IEEE Trans. Circuit Theory 18, 507 (1971).

## Slide 14
Hewlett Packard Labs is kicking off an exciting 12-part lecture series with the world-renowned Professor Leon Chua – accomplished IEEE Fellow, Professor of Electrical Engineering and Computer Sciences at UC Berkeley, and a pioneer in neural network and Memristor research.
Over the course of the 12 weekly lectures, Professor Chua will offer a peek into his life’s work exploring distinct research areas which have emerged from highly nonlinear and dynamical phenomena including: Memristors, Cellular Nonlinear Networks (CNN), The Local Activity Principle and the Edge of Chaos.
Don’t miss this rare opportunity to hear from one of the greatest thought leaders of our industry. ‘Linearize then analyze’ is no longer valid for understanding nanodevices or neurons – a new mathematical theory of electronics is needed, and was developed 35 years ago!
Event details:
What: Chua Lecture Series
When: Every Tuesday starting September 8 through November 24, 10:30 a.m. – 12:00 p.m. Pacific Time
How to attend: Register here – Attend in person or on the web.
We highly recommend that you take the opportunity to hear the Professor Chua lectures in person at Building 20 Auditorium in Palo Alto.
Register for upcoming lecture and scroll down the registration page to sign up for the entire lecture series. This is open to everyone so feel free to share this event with your colleagues, friends and social networks!

## Slide 15
Sung Hyun Jo, et al. Nano Lett. 10, 1297 (2010)
Viable path toward scalable biomimetic computing?
Neuron (neuristor)
Locally active memristors
Captures key features of the brain:
1) Non-linear dynamics (“edge of chaos”) of neurons
2) High density architecture, localized memory
i.e. not the von Neuman architecture with physically separated compute and memory !
3) Massive parallelism
Synapse
Nonvolatile memristors

## Slide 16: Accelerates many workloads FFT, Metropolis-Hastings, Simulated Annealing
Analog applications of nonvolatile memristors
Memristor array = matrix Gij
Computes Matrix-vector dot product VI * G in one time step
Requires non-binary states for each memristor

## Slide 17
200 μm
Real-time Oscilloscope
Coplanar Waveguide
Need for high speed dynamic electrical testing
Top Electrode
Bottom Electrode
Memristor
Fast pulse generator
> 30 GHz bandwidth
A. C. Torrezan, et al., Nanotechnology, 22, 485203 (2011)
J. P. Strachan, et al., Nanotechnology, 22, 505402 (2011)

## Slide 18
~100 ps ON and OFF switching in TaOx

## Slide 19
TiO2
Pt
An accurate, predictive circuit model needs a good microphysical model
Key questions:
What are the important physical processes involved in switching (heating, drift, diffusion)?
Role of oxygen vacancies (n-type dopants), electromigration, dielectric breakdown, migration of the metal electrode atoms? Metal/oxide schottky-barrier physics, electrochemistry, etc.
Approach: materials/device characterization + electrical modeling
Pt
20 nm
-
+
V
30nm – 10μm
Understanding Memristor Microphysics

## Slide 20: Getting nanoscale chemical resolution: STXM at the Advanced Light Source, Berkeley
Scanning Transmission X-ray Microscope (STXM)
Spatial resolution down to 25nm
Probes entire depth of sample
Energy resolution (70 meV) for chemical identification

## Slide 21: X-ray spectromicroscopy and TEM of TiO2 NV memristor
Devices fabricated atop thin Si3N4 windows
Window
Allows:
1. Non-destructive characterization (no delamination or cross-sectioning)
2. X-ray or Electron microscopy of same device
3. In-situ electrical addressing of device during characterization
Photograph of actual device
2009

## Slide 22
455
460
465
470
0
2
4
6
8
X-ray energy (eV)
Absorption (a.u.)
Chemical/Structural Mapping by XAS
Diffraction pattern identifies the reduced phase as crystal Ti4O7
TEM - Electron diffraction
Ti4O7 is:
Stable sub-oxide of TiO2
Member of TinO2n-1 Magneli phases
Metal-Insulator Transition 140-150K
TiO2 Anatase
TiO2 Amorphous
TiO2-x Reduced
J.P. Strachan, M.D. Pickett, J.J. Yang, S. Aloni, A.L.D. Kilcoyne, G. Medeiros-Ribeiro, R.S. Williams, Advanced Materials 22, 3573 (2010)

## Slide 23: Ramifications of the X-ray characterization
Deliberately engineer devices with Ti4O7 layer from the beginning to eliminate “electroforming”
Broad range of stable phases TinO2n-1 for n>2, suggests many “intermediate states” can form, limits cycling endurance
Pt / 35nm “Ti4O7” / 5nm TiO2 / Pt
TiO2
Pt
Pt
Ti4O7
Yielded lower voltage operation and lower variability
TaOx
TiO2
Simpler phase diagram of TaOx system 106  1012 endurance

## Slide 24
X-ray intensity
2 μm
ION
IOFF
ln (IOFF/ION)
ΔOD
0
+0.05
-0.05
Device
pulses
0
t
Gating
pulses
X-ray
pulses




ON
OFF

Only imaging device states with
GON > 1.5e-4 S (~ 6 kΩ)
GOFF < 1.5e-5 S (~66 kΩ)
ON
OFF
Within crosspoint area, AbsOFF - AbsON = +0.0015 ± 0.0002 (SNR ≈ 7)
Outside of crosspoint area, No signal above noise level
Despite large conductance change, material changes are extremely small and no localization observed for small power operation
in operando analysis of TaOx
Applied roughly +1.25 V, -2.0 V
2015

## Slide 25
Spectroscopy of device regions: field and temperature effects
X-ray intensity
2 μm
“bright” region
“dark” region
Additional experiment: Apply +V vs 0V and look for Joule heating
Thermal effects seen in bright region – localized current flow in bright region only!

## Slide 26
Ti4O7 Metal-Insulator Transition 140-150K
Lakkis et. al, PRB, (1976)
Many metal-oxides exhibit Mott Transitions
Correlated-electron insulator to conductor phase change The basis for a locally active memristor

## Slide 27: Identification of local activity (NDR) in Ti4O7
Metal-Insulator transitions in metal oxides provide a new functionality we can exploit
Presence of Ti4O7 explains Negative Differential Resistance effect
Current through device  Joule heating  growing metallic phase within Ti4O7
M. D. Pickett, et al. Advanced Materials, (2011)
Data
Simulation
Data
Simulation

## Slide 28
NbO2 Locally Active “Mott” Memristor – thermoelectric switching
Oscillator with DC bias!
rch =
30 nm

## Slide 29
Leon Chua’s Version of the Hodgkin-Huxley Model
L. Chua et al., “Hodgkin-Huxley Axon is made of Memristors,”
International Journal of Bifurcation and Chaos 22 (2012) art. # 1230011.

## Slide 30: A Neuristor inspired by the Hodgkin-Huxley model
M. D. Pickett, et al, Nature Materials 12, 114 (2013).
Implements “All or Nothing” spiking:
1000 times faster than a neuron
1% of the energy of a neuron

## Slide 31
Neuristor Spiking
emulates signals
seen in brains
“Regular Spiking”
C1=5.1 nF, C2=0.75 nF
“Fast Spiking”
C1=1.6 nF, C2=0.5 nF
“Chattering”
C1 = 5.1 nF, C2 = 0.5 nF
Compared to brain
500x frequency
4x V amplitude
1 % of energy/spike

## Slide 32: Drove our research into phase transition materials/devices
In VO2, local heating drives Mott-Peierls transition = locally active memristor
Identified two unknown metastable phases!
X-ray structural and electronic mapping shows the Mott and Peierls transitions are not simultaneous
S. Kumar, et al., Advanced Materials, (2014)
Measure T also!

## Slide 33
Dark field cross-sectional TEM image of NbOx memristor. The heated region is thermally connected to Tamb through the effective thermal resistance, Rth, and thermal capacitance, Cth.
Integrated Mott memristors – thermoelectric design
RthCth ≤ 0.1 ns
Rth ≥ 106 K/W
Cth ≤ 10-16 J/K
10x faster
0.1x energy
of previous device
Ce
SiO2
W bottom electrode
SiNx
Pt top electrode
TiN
TiN
Nanovia
NbOx
Tamb
TN
Rth
Cth
≤ 0.1 nF

## Slide 34
New NbO2 memristor displays oscillatory and chaotic behavior
Oscillations
Oscillations
DC characteristics
1.20 V
0.96 V
1.03 V
1.00 V
R1=1kΩ
C1=1nF
C2
M
R2
Oscillations and chaos depend sensitively on DC bias

## Slide 35
in situ and in operando analysis of a circuit.
Applied voltages induce local heating and field-effects modifying structure and composition at the nanoscale
Next step: from individual device to an entire (model) circuit

## Slide 36: Further applications of SR for circuit analysis
Mapping of chemical/structural/electronic properties
~5 nm in situ spatial and ~1 ns in operando temporal resolution
Coherence enables 3D analysis
As devices scale down in size, interfaces and sidewalls dominate the properties
Interfaces with top and bottom electrodes affect the electronic properties
Sidewall reactions with interlayer dielectric (ILD) can create “dead” zones or shunting paths
Vacancy/oxygen diffusion can limit cycling lifetimes
M2
M1
Bit
Via

## Slide 37: Some thoughts on ALS applications for computing
Driving “More than Moore” functionality for neuromorphic computing
  Semiconductor size scaling will eventually reach 5 nm – need to look inside the devices
  Fundamental shift: New devices are now viable to complement CPUs (hardware accelerators)
   Exploration of novel devices and functionalities integrated on top of CMOS
  Chemical/electronic/structural information at these length scales is a critical need
  Brightness is the compelling feature that allows mapping
  Opens up “material discovery” rather than just heroic device characterizations
  Our research at ALS led to fundamental materials understanding, which enabled the discovery of ‘locally active’ Mott memristors and in turn the invention of a solid-state neuristor

## Slide 38
Acknowledgements for SR studies
Molecular Foundry, Berkeley
Shaul Aloni
Advanced Light Source, Berkeley
David Kilcoyne
Andreas Scholl
Tolek Tyliszczak
Advanced Photon Source, Argonne
Martin Holt
Volker Rose
HP
John Paul Strachan
Suhas Kumar
Cat Graves
Gary Gibson
Miao Hu
Warren Jackson
Emma Merced
Feng Miao
Matthew Pickett
Antonio Torrezan
Jianhua Yang
Max Zhang
Tel-Aviv University
Ilan Goldfarb
UC Santa Barbara
Dima Strukov

## Slide 39: Neuro challenges a larger community than just nano
Need to go beyond NNI and involve diverse creative communities
Information technology requires a system-level awareness: Architecture
  Nano devices and circuits will be necessary, but not sufficient for a paradigm shift
  Also need insights from neurophysiology (circuits) and psychology (algorithms)
Revolutionary advances disguised as evolutionary to gain market acceptance
  A new nanodevice is useless if it requires a major change (i.e. expense) to a system or to manufacturing processes (customers don’t pay for performance – they expect it)
  Two-thirds (or more) of any computing system today is design and software
Avoid fads and bandwagons (e.g. Graphene and Deep Learning)
  Need a broad investment portfolio of competing technologies and ideas
Multi-disciplinarity is essential – need experts in each domain who can communicate, not lots of broad but shallow neophytes